LIGHT SODA ASH

Description:

White, powder, hygroscopic, easily dissolved in water, clear and colorless in water solution material. Main compound is Sodium Carbonate.
Standart No: TS 525 TYPE 3B

Chemical Specifications: Sodium Carbonate, (Na2CO3) (%) 99,10 min. Sodium Chloride, (NaCl) (%) 0,25 max. Iron, (Fe) (ppm) 15 max. Insoluble matter in water (%) 0,01 max. Sulfate, SO42- (%) 0,027 max. Physical Specifications: Structure of the Material Free flowing powder Standard density 0,47 - 0,59 gr/cm3

Packaging:

In block-bottom laminated polypropylene (PP) bags of 25 or 50 kgs. each.

Palletized and shrink-wrapped 1000 kg. each, containing 25 kg. laminated block-bottom PP bags.

In polypropylene big-bags with polyethylene (PE) in-liner and four loops, 650 or 1000 kgs. each.

In bulk